## Slide 1: Course C.03.06.01 Aggregate – gradation analysis
Marek Pszczola
(presentation was prepared on the basis of lectures prof. S. Romanoschi, USA)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 4: Types of Gradations
* Uniformly graded
- Few points of contact
- Poor interlock (shape dependent)
- High permeability
* Well graded
- Good interlock
- Low permeability
* Gap graded
- Only limited sizes
- Good interlock
- Low permeability

## Slide 5: Aggregate Gradation
Use 0.45 Power Gradation Chart
Blend Size Definitions
  maximum size
  nominal maximum size
Gradation Limits
  control points
  restricted zone

## Slide 6: 0.45 Power Grading Chart
Example:
4.75 mm sieve plots at (4.75)0.45 = 2.02
Sieve Size (mm) raised to 0.45 Power
0
20
40
60
80
100
0
1
2
3
4
Percent Passing
Notes: To specify gradation the HMA industry uses a .45 power graph. It is a modification of the Fuller’s curve used by geotechnical engineers - rather than use a power of 0.50 it uses a 0.45 for the exponent in the equation.

## Slide 7: 0.45 Power Grading Chart
0 .075 .3 .6 1.18 2.36 4.75 9.5 12.5 19.0
Sieve Size (mm) Raised to 0.45 Power
0
20
40
60
80
100
maximum density line
Percent Passing
max
size
Notes: The maximum density gradation (line) represents a gradation in which the aggregate particles fit together in their densest possible arrangement. This is not the most desirable gradation for HMA because there would be very little aggregate space within which to develop sufficiently thick asphalt films for a durable mixture.

## Slide 8: Aggregate Size Definitions
Nominal Maximum Aggregate Size
  one size larger than the first sieve to retain more than 10%
Maximum Aggregate Size
  one size larger than nominal maximum size
100
100
90
72
65
48
36
22
15
9
4
100
99
89
72
65
48
36
22
15
9
4
Notes: For HMA pavements these are the definitions for gradations.

## Slide 9: 0.45 Power Grading Chart
100
0
.075 .3 2.36 4.75 9.5 12.5 19.0
Percent Passing
control point
restricted zone
max density line
max
size
nom
max
size
Sieve Size (mm) Raised to 0.45 Power
Notes: To specify aggregate gradation, two additional features are added to the 0.45 chart: control points and a restricted zone. Control points function as master ranges through which gradations must pass. They are placed on the nominal maximum size, an intermediate size and the dust size.
The restricted zone resides along the maximum density gradation between the intermediate size (either 4.75 or 2.36 mm) and the 0.3 mm size. It forms a band through which gradations should not pass. Gradations that pass through the restricted zone have often been called “humped gradations” because of the characteristic hump in the grading curve that passes through the restricted zone. In most cases, a humped gradation indicates a mixture that possesses too much fine sand in relation to total sand. This gradation practically always
results in tender mix behavior, which is manifested by a mixture that is difficult to compact during construction and offers reduced resistance to permanent deformation during its performance life. Gradations that violate the restricted zone possess weak aggregate skeletons that depend too much on asphalt binder stiffness to achieve mixture shear strength. These mixtures are also very sensitive to asphalt content and can easily become plastic.

## Slide 10: Superpave Aggregate Gradation
100
0
.075 .3 2.36 12.5 19.0
Percent Passing
Design Aggregate Structure
Sieve Size (mm) Raised to 0.45 Power
Notes: The term used to describe the cumulative frequency distribution of aggregate particle sizes is the design aggregate structure. A design aggregate structure that lies between the control points and avoids the restricted zone meets the requirements of Superpave with respect to gradation. Superpave defines five mixture types as defined by their nominal maximum aggregate size:

## Slide 11: Superpave Mix Size Designations
Superpave Nom Max Size Max Size
Designation (mm) (mm)
37.5 mm 37.5 50
25 mm 25 37.5
19 mm 19 25
12.5 mm 12.5 19
9.5 mm 9.5 12.5
Notes: These are the five gradations developed for Superpave.

## Slide 12: Gradations
* Considerations:
- Max. size < 1/2 AC lift thickness
-
Larger max size
+ Increases strength
+ Improves skid resistance
+ Increases volume and surface area of agg which decreases required AC content
+ Improves rut resistance
+ Increases problem with segregation of particles
- Smaller max size
+ Reduces segregation
+ Reduces road noise
+ Decreases tire wear
Notes: Several factors need to be considered in selecting a desirable aggregate gradation. The maximum size of the aggregate needs to be at a minimum less than one half of the planned lift thickness. Current construction practices with Superpave gradations indicate that this needs to be changed to less than one-third of the lift thickness.
Larger maximum size aggregate gradations have several advantages such as improved aggregate interlock, improved skid resistance and improved rut resistance. Local availability of aggregates will usually dictate the largest size aggregate. Also, the larger maximum size gradations also tend to have more problems with gradation separation (segregation) during construction.

## Slide 13: Target Gradation
Acceptable gradation band specified
Mix design selects a job mix formula (JMF) which falls within band and meets design criteria
Superpave
  5 nominal sizes (37.5, 25, 19, 12.5, and 9.5 mm)
  Four sieve sizes used to set upper and lower limits
  Staying out of the restricted zone is suggested to minimize problems with natural sands
Notes: Target gradations are usually selected to meet an agency-specified gradation band. The selected gradation needs to meet the agency requirements as well as all other Superpave gradation and aggregate requirements.
At the present time, there are 5 Superpave gradation bands. Each uses 4 sieve sizes to set upper and lower limits on the gradation.
The restricted zone was originally included to help eliminate rounded natural sands. However, with the requirements on fine aggregate angularity, the need to stay out of the restricted zone is evaluated on a case by case basis (historical experience).

## Slide 14: Blending Stockpiles
Basic formula for combining stockpiles to achieve a target gradation is:
p = Aa + Bb + Cc + ….
where:
p = percent of material passing given sieve size
A, B, C, .. = percent passing given sieve for each agg.
a, b, c, … = decimal fraction of A, B, C, … to be used
Notes: Once a target gradation or gradation band is selected, percentages of the aggregate stockpiles needed to produce an acceptable gradation are determined.
This is usually accomplished using a spreadsheet and a trial and error approach.

## Slide 15: Blending Stockpiles
Plot individual gradations
Plot specification limits
Can be used for initial assessment
  Can blend be made from available materials?
  Identification of critical sieves
  Est. trial proportions
Notes: The ability of a given set of aggregate stockpiles to meet particular gradation band requirements can be initially assessed by plotting the individual stockpile and gradation band requirements

## Slide 16: All possible combinations fall between A and B
0.075 0.3 1 .18 4.75 9.5 12.5 19
Sieve Size, mm
Percent Passing, %
Control points for
12. 5 nominal max. size
Gradation A
Gradation B
Notes: If the individual gradations bracket the gradation band, then it is possible to produce a combined gradation which will be within the gradation band. Determining the percentages will be a trial and error process.

## Slide 17: No poss. combination of A and B will meet spec.
0.075 0.3 1 .18 4.75 9.5 12.5 19
Sieve Size, mm
Percent Passing, %
Control points for
12. 5 nominal max. size
Gradation A
Gradation B
Notes: If the individual stockpile gradations are both either above or below the target gradation band, then there is no combination of the stockpiles which will produce an acceptable gradation.

## Slide 18: All poss. combinations pass through the cross-over point Blends containing more A than B will be closer to A
0.075 0.3 1 .18 4.75 9.5 12.5 19
Sieve Size, mm
Percent Passing, %
Control points for
12. 5 nominal max. size
Gradation A
Gradation B
Notes: If the individual stockpile gradations cross, then the any combination of these stockpiles will have that same percentage for that particular sieve size.

## Slide 19: Trial and Error Steps
Select critical sieves in blend
Determine initial proportions which will meet critical sieves
Check calc. blend against specification
Adjust if necessary and repeat above steps
Notes: Once it has been established that an acceptable gradation can be prepared using the designated stockpiles, these steps need to be followed to determine the desired percentages of each stockpile.

## Slide 20: Blended Aggregate Specific Gravities
Once the percentages of the stockpiles have been established, the combined aggregate specific gravities can also be calculated
Notes: Remember, two specific gravity tests are needed. The results from these two tests need to be combined to obtain the specific gravity of the composite.

## Slide 21: Combined Specific Gravities
G =
1
P1 + P2 + ……. Pn
100 G1 100 G2 100 Gn
Notes: This is the equation used for combining aggregate properties.

## Slide 22: Blending of Aggregates
Reasons for Blending
  Obtain desirable gradation
  Single natural or quarried material not enough
  Economical to combine natural and process materials
Notes: We blend aggregates for these reasons.

## Slide 23: Blending of Aggregates
Numerical Method
  Trial and Error
  Basic Formula
Notes: There are two methods for blending aggregates. The most common is trial and error. The basic formula is not used.

## Slide 24: Blending of Aggregates
P = Aa + Bb + Cc + ….
  Where:
  P = % passing a given sieve for blended aggregates A, B, C, …
  A, B, C, … = % material passing a given sieve for each aggregate A, B, C, …
  a, b, c, … = Proportions (decimal fractions) of aggregates A, B, C, … to be used in blend
Notes: This is the basic formula for blending.

## Slide 25: Blending of Aggregates
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% Used
U.S. Sieve
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
90
30
7
3
1
0
0
100
100
100
88
47
32
24
10
100
Notes: Example. Starting with two aggregates.

## Slide 26: Blending of Aggregates
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% Used
U.S. Sieve
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
45
15
3.5
1.5
0.5
0
0
100
100
100
88
47
32
24
10
100
50 %
50 %
First Try
(remember trial & error)
90
30
7
3
1
0
0
50
90 * 0.5 = 45
30 * 0.5 = 15
7 * 0.5 = 3.5
3 * 0.5 = 1.5
1 * 0.5 = 0.5
0 * 0.5 = 50
0 * 0.5 = 0
100 * 0.5 = 50
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
Notes: The first trial we will use 50% of each pile.

## Slide 27: Blending of Aggregates
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% Used
U.S. Sieve
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
45
15
3.5
1.5
0.5
0
0
100
50
50
44
23.5
16
12
5
50
50 %
50 %
90
30
7
3
1
0
0
50
95
65
47.5
25
16.5
12
5
100
100
100
88
47
32
24
10
100
Notes: This worked but the No. 50 sieve and the No 100 sieve are low.

## Slide 28: Blending of Aggregates
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% Used
U.S. Sieve
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
45
15
3.5
1.5
0.5
0
0
100
50
50
44
23.5
16
12
5
50
50 %
50 %
90
30
7
3
1
0
0
50
95
65
47.5
25
16.5
12
5
100
100
100
88
47
32
24
10
100
Let’s Try
and get
a little closer
to the middle of
the target values.

## Slide 29: Blending of Aggregates
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% Used
U.S. Sieve
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
27
9
2.1
0.9
0.3
0
0
100
70
70
61.6
32.9
22.4
16.8
7
70
70 %
30 %
90
30
7
3
1
0
0
30
97
79
63.7
33.8
22.7
16.8
7
100
100
100
88
47
32
24
10
100