## Slide 1: Course C.03.06.01 Aggregates – laboratory tests
Marek Pszczola
(presentation was prepared on the basis of lectures prof. S. Romanoschi, USA)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 4: 4 Steps of Superpave Mix Design
1. Materials Selection
2. Design Aggregate Structure
3. Design Binder Content
4. Moisture Sensitivity
TSR

## Slide 5: Aggregate Properties
Consensus Properties - required
  coarse aggregate angularity (CAA)
  fine aggregate angularity (FAA)
  flat, elongated particles
  clay content
Source Properties - agency option
  toughness
  soundness
  deleterious materials

## Slide 6: Fine Aggregate Angularity
Measured on - 2.36 mm Material
Based on Air Voids in Loose Sample
AASHTO T 304
Requirements Depend on
  depth of layer within pavement
  traffic level

## Slide 7: Fine Aggregate Angularity
fine aggregate sample
cylinder of known volume (V)
uncompacted voids =
V - M / Gsb
V
x 100%
funnel
M
measured
mass

## Slide 9: Fine Aggregate Angularity
Traffic Depth from Surface
ESALs < 100 mm > 100 mm
. . .
10 - 30 x 10 6 45 40
. . .
. . .
% air voids in loose sample
> Rounder particles pack tighter together -- less air
Minimum

## Slide 10: Coarse Aggregate Angularity
Measured on + 4.75 mm material
Based on Fractured Faces
  fractured surface larger than 25% of aspect ratio
ASTM D 5821
Spec Requirements Depend on
  depth of layer within pavement
  traffic level

## Slide 14: Coarse Aggregate Angularity
Traffic Depth from Surface
ESALs < 100 mm > 100 mm
. . .
10 - 30 x 10 6 95/90 80/75
. . .
. . .
95% one fractured face
90% two+ fractured faces
Minimum

## Slide 15: Flat, Elongated Particles
Measured on + 4.75 mm Material
Based on Dimensional Ratio of Particles
  ratio of max to min dimension < 5
ASTM D 4791
Requirements Depend on
  traffic level

## Slide 16: Flat, Elongated Particles
1:5 pivot point
swinging arm
fixed post (A)
fixed post (B)

## Slide 21: Flat, Elongated Particles
Traffic
ESALs Percent
. .
10 - 30 x 10 6 10
. .
. .
percentage
of flat and elongated particles
Maximum
5
1

## Slide 22: Clay Content
Measured on - 4.75 mm Material
Based on Sand Equivalent Value
AASHTO T176
Requirements Depend on traffic level
> How dirty is the sand ?

## Slide 25: Clay Content
suspended clay
sedimented aggregate
clay reading
sand reading
graduated
cylinder
flocculating
solution

## Slide 26: Clay Content
Traffic
ESALs Percent
. .
10 - 30 x 10 6 45
. .
. .
Sand Equivalent value
Minimum
> More sand - Less clay
Clay on aggregate particles
reduces binder adhesion

## Slide 28: Methylene Blue Test

## Slide 29: Methylene Blue Results
Methylene Blue Expected Performance
(mg/g)
5 - 6 Excellent
10 - 12 Marginally acceptable
16 - 18 Problems or possible failure
20+ Failure

## Slide 30: Aggregate Source Properties
Toughness
  AASHTO T96 (LA Abrasion)
Soundness
  AASHTO T104 (Na or Mg Sulfate Soundness)
Deleterious Materials
  AASHTO T112 (Clay Lumps and Friable Particles)
Others selected by Agency
> Used in Mix Design or for Acceptance Control

## Slide 31: Toughness
AASHTO T 96 or ASTM C131, C535
Los Angeles Abrasion Test
Typical values range 20 to 55%
Specifications usually require 45% or less

## Slide 32: Toughness
5000 gm of aggregate with 6 to 12 two inch steel balls is tumbled for 500 revolutions.
The test is run on a graded aggregate sample.
The amount of material passing the No. 12 sieve is weighed and the percent loss is determined.

## Slide 33: Los Angeles Abrasion Machine

## Slide 37: Toughness
Source of requirement:
  Past experience (43%)
  Unaware of origin (25%)
  Adopted from ASTM, AASHTO or FHWA (28%)
  Conducted research to establish value (4%)

## Slide 38: L.A. Abrasion - Typical values
Basalt 10 to 17%
Dolomite 18 to 30%
Gneiss 33 to 57%
Granite 27 to 49%
Limestone 19 to 30%
Quartzite 20 to 35%

## Slide 39: Sulfate Soundness
AASHTO T 104
Sodium or Magnesium sulfate soundness test
Typical values range 10 to 20% loss

## Slide 40: Sulfate Soundness
The sample is submerged for 18 hours in a sulfate solution
It is removed and dried @ 230 F
The process is repeated usually five times (cycles)

## Slide 41: Sulfate Soundness
54 % of states use sodium
  Range of values is 5 to 25% with the majority at 12 or 15
19 % of states use magnesium
  Range of values is 10 to 30% with the majority at 15 or less

## Slide 42: Sulfate Soundness
Before
After

## Slide 43: Deleterious Materials
Percentage of contaminants such as shale, wood, mica and coal
Measured by AASHTO T 112, “Clay Lumps and Friable Particles in Aggregates.”
Determined by wet sieving the material
Requirements range from 0.2 percent to 10 percent