## Slide 1: Course C.03.06.02 Portland Cement Concrete (PCC) Pavements
Marek Pszczola
(presentation was prepared on the basis of lectures prof. S. Romanoschi, USA)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 5: Paver Set-Up
Square up paving kit
Check pan for trueness
Adjust pan for crown
Adjust pan attitude (draft)

## Slide 7: Extrusion Envelope
Profile Pan
Tamper
Vibrator
Strike Off
Concrete Head
Profile Pan Batter -
Compression-Paver Uplift
Fluidized
Concrete
Side Form Resistance Batter
Excess Concrete
Movement

## Slide 8: Paver Sensor System
Check thoroughly
Set wands same distance apart
Set wands level
Set counterbalance

## Slide 21: Texturing - Tining
Longitudinal
Transverse
Spacing of ¾ in (20 mm) or less
Random tine spacing

## Slide 25: Headers
Use fresh concrete
Consolidate thoroughly
Straight edge
Stringline
Edge tool
Texture and cure in a timely manner

## Slide 32
Extreme Weather Placement
Specifications will include high and low temperatures at which precautions must be taken to protect new concrete

## Slide 33
Hot Weather Placement Considerations
Control temperature of PCC mix
Use set retarders
Timely sawing
Fog new pavement (until sawing completed)

## Slide 35
Cold Weather Placement
Use set accelerators
Cover new pavement
  Polyethylene sheeting
  Straw
  Curing blankets

## Slide 37
Poor Placement Practice
Excess PCC at auger
"Station dumping" difficult to control
PCC has very low slump and appears to be slightly segregated

## Slide 39: Tearing of the Mix
Check:
Speed of paver
Square of paving kit to stringline
Vibration frequency
Draft of the pan
Mix proportions
Air content
W/C ratio

## Slide 41: Too Much Grout on Surface
Too much water applied to surface
Over-vibration (vibration speed too high)
Machine moving too slow for vibration
Rain!

## Slide 45
Trackline and Stringline
A clean trackline helps in constructing a smooth pavement
Protect the stringline from displacement
Avoid knots in the stringline

## Slide 49
Maintain Equipment
Repair hydraulic leaks
Use proper replacement parts
Clean up after each use
  Don't create soft spots in base
Other

## Slide 51: Vibrator Streaking
Check:
Head above vibrators
Materials and mixtures
Frequency
Paver speed
Vibrator positions and spacing
Blown vibrator

## Slide 53
Edge Slump
Verify consistency of PCC
  Slump
  Air
  Gradation
Paver edge overbuild

## Slide 56: Variation in Texturing
Review mixing and batching operations
Check placing and finishing process
Observe operation of tining equipment
Check tining equipment trackline
Check vibrator positioning and operation
Other

## Slide 59: Verify Thickness
Probe concrete for thickness
Check surface for specified profile

## Slide 60: Summary
High-quality PCC pavement is achieved with:
Accurate line and grade control
Uniform, well compacted grade
Consistent PCC production and delivery
Consistent, uninterrupted forward motion of paver
Adequate internal vibration
Timely texturing and curing