## Slide 1: Course C.03.06.02 Maintenance – Introduction
Marek Pszczola
(presentation was prepared on the basis of lectures prof. S. Romanoschi, USA)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 4: Steps In The Rehabilitation Process
Pavement
Data
Collection
Project
evaluation
Select
feasible
alternatives
Reconstruction
Restoration
Recycling
Resurfacing
Life - cycle
costs
Non-
monetary
factors
Select
preferred
alternatives
Detailed
PS & E
Construction
Monitor
Performance

## Slide 5: Definitions
Pavement maintenance
Pavement rehabilitation

## Slide 6: Network Condition and Rehabilitation Timing
12% OF
LIFE
EXCELLENT
GOOD
FAIR
POOR
VERY POOR
FAILED
40% DROP
IN QUALITY
40% DROP
IN QUALITY
75% OF LIFE
$1.00 FOR
RENOVATION HERE
WILL COST
$4.00 TO $5.00
HERE
TIME

## Slide 7: Functions of Surface Treatments
Provide a new wearing surface
Seal cracks in the surface
Waterproof the surface
Improve pavement surface friction and
surface drainage

## Slide 8: Functions of Surface Treatments
Slow pavement weathering and aging
Improve the surface appearance
Provide visual delineation as between the
mainline pavement and the shoulder

## Slide 9: Definitions
Surface application of asphaltic material with or without aggregate
  Fog seal
  Sand seal
  Asphalt chip seal
  Slurry seal
  Micro-surfacing
  Cape seal

## Slide 10: Fog Seal

## Slide 11: Asphalt Chip Seal

## Slide 12: Asphalt Application

## Slide 13: Rock Application

## Slide 14: Rolling

## Slide 15: Design Problems - Asphalt Chip Seals

## Slide 16: Slurry Seal

## Slide 17: Micro-Surfacing

## Slide 18: Rut Fill

## Slide 19: Cape Seal

## Slide 20: Cost Considerations
Typical surface treatment costs
  Chip seal $0.90 /m²
  Db. chip seal $1.35 /m²
  Slurry seal $0.84 to $1.14 /m²
  Micro-surfacing $1.05 to $2.00 /m²
  Fog seal $0.12 to $0.17 /m²
  Sand seal $0.30 to $0.48 /m²
  Cape seal $1.70 to $2.40 /m²

## Slide 21: City of Albuquerque (1999) - Costs
Mill & Inlay $5.80 per sq. yd.
Polymer modified
Slurry Seal $1.25 per sq. yd.
Crack sealant $0.61 per sq. yd.
In-house Chip seal $0.90 per sq. yd.
Fog Seals $0.15 per sq. yd.

## Slide 22: Hot-Mix Asphalt Overlays

## Slide 23: Introduction
Most popular method
Relatively fast and cost-effective means for:
  Correcting deficiencies
  Restoring user satisfaction
  Adding structural capacity
Poor performance is NOT uncommon

## Slide 24: Pre-Overlay Treatment and Repair
Dependent upon:
  Type of overlay
  Structural adequacy of existing pavement
  Existing types of distress
  Future traffic
  Physical constraints
  Cost

## Slide 25: Pre-Overlay Treatment and Repair

## Slide 26: Localized Repair
Repair
cost
Overlay
cost
% Area repaired

## Slide 27: Influence of Repairs on Design Overlay Thickness
% of Area Repaired
Total
Cost
Minimum
Total Cost
Optimum

## Slide 28: Controlling Reflection Cracking
Geotextiles or fabrics
Stress relieving or stress absorbing
membrane interlayers
“Band aid” type crack sealants

## Slide 29: Overlay Thickness
  Engineering judgement
  Deflection approach
  Structural deficiency
  Mechanistic approach

## Slide 30
HMA Overlays of Concrete
Pavements

## Slide 31: Design Issues
Rate of propagation through overlay
Number of reflected cracks
Rate of deterioration of reflected cracks
Amount of water that can infiltrate through
the cracks

## Slide 32: Reflection Crack Control Measures
Fabrics
Stress-relieving interlayers
Crack-arresting interlayers
Preoverlay treatments
Slab repair or replacement
Sawing and sealing joints
Increased overlay thickness

## Slide 33: Crack Control Effectiveness
Delay the occurrence of cracking
Reduce the number of cracks
Control the crack severity
Provide other benefits
  Reduce overlay thickness
  Enhance waterproofing capabilities

## Slide 34: Fabric Application

## Slide 35: Fabric Application

## Slide 36: Stress-Absorbing Interlayers

## Slide 37: Reduction in Reflection Cracking
Material
Trans.
Long.
Polyguard 665
35 %
0.3 %
Royston #108
90 %
0 %
Royston #10AR
35 %
0 %
PavePrep
5 %
2 %
Roadglas
29 %
0 %
Biuthene
H.D.
50 %
0 %
Petrotac
30 %
0 %

## Slide 38: Preoverlay Repairs
Slab stabilisation
Fractured slabs
Slab repair/replacement
Load transfer restoration

## Slide 39: Fractured Slab Techniques
Crack and seat (JPCP)
Break and seat (JRCP)
Rubblize (JPCP, JRCP, CRCP)

## Slide 40: Cracking and Seating
Shortens effective slab length
Standard practice in many States
Not “generally” recommended for use on poor subgrades
Design methods (overlay thickness)

## Slide 41: Cracking and Seating

## Slide 42: Cracking and Seating

## Slide 43: Cracking and Seating - crack pattern

## Slide 44: Cracking and Seating

## Slide 45: Rubbilization
Total destruction of the slab action
Pavement is broken into individual pieces ranging from aggregate size to a maximum of 6 to 12 inches
Compaction can be obtained by several passes of a 10 ton steel wheel roller or vibratory roller
Structual coefficient is 0.28.

## Slide 46: Rubblization

## Slide 47: Rubblization

## Slide 48: Sawing and Sealing Joints
Concede appearance of reflection cracking
Objective: control rate of deterioration
Reduces spalling of reflection cracks
Candidates should have well-defined joints
Sawcut must be directly above the underlying joint

## Slide 49: Sawing and Sealing Joints

## Slide 50: Increased Overlay Thickness
Delays the occurrence of reflection cracking
Cracks propagate about 25 mm per year
Reduces temperature fluctuations in underlying pavement