## Slide 1: Cours C.03.06.01 Granulats – analyse granulométrique
Marek Pszczola
(présentation préparée sur la base des cours du prof. S. Romanoschi, États-Unis)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 4: Types de granulométries
* Uniformee granulométrie
- Peu points de contact
- Faible s’imbriquent (Forme dependent)
- Élevée perméabilité
* Bien granulométrie
- Bonne s’imbriquent
- Faible perméabilité
* Discontinue granulométrie
- Only limiteées dimensions
- Bonne s’imbriquent
- Faible perméabilité

## Slide 5: Granulométrie des granulats
Utiliser 0.45 Power granulométrie Diagramme
mélange dimension Définitions
  dimension maximale
  dimension nominalese maximale
granulométrie Limites
  points de contrôle
  zone restreinte

## Slide 6: Diagramme granulométrique à puissance 0,45
Exemple :
4.75 mm tamis plots at (4.75)0.45 = 2.02
tamis dimension (mm) raised à 0.45 Power
0
20
40
60
80
100
0
1
2
3
4
Pourcentage passant
Notes: To specify gradation the HMA industry uses a .45 power graph. It is a modification of the Fuller’s curve used by geotechnical engineers - rather than use a power of 0.50 it uses a 0.45 for the exponent in the equation.

## Slide 7: Diagramme granulométrique à puissance 0,45
0 .075 .3 .6 1.18 2.36 4.75 9.5 12.5 19.0
tamis dimension (mm) Raised à 0.45 Power
0
20
40
60
80
100
ligne de densité maximale
Pourcentage passant
max
dimension
Notes: The maximum density gradation (line) represents a gradation in which the aggregate particles fit together in their densest possible arrangement. This is not the most desirable gradation for HMA because there would be very little aggregate space within which to develop sufficiently thick asphalt films for a durable mixture.

## Slide 8: Définitions des dimensions des granulats
Dimension nominale maximale du granulat
  une dimension au-dessus du premier tamis retenant plus de 10 %
Dimension maximale du granulat
  une dimension au-dessus de la dimension nominale maximale
100
100
90
72
65
48
36
22
15
9
4
100
99
89
72
65
48
36
22
15
9
4
Notes: For HMA pavements these are the definitions for gradations.

## Slide 9: Diagramme granulométrique à puissance 0,45
100
0
.075 .3 2.36 4.75 9.5 12.5 19.0
Pourcentage passant
Contrôler point
zone restreinte
max densité ligne
max
dimension
nom
max
dimension
tamis dimension (mm) Raised à 0.45 Power
Notes: To specify aggregate gradation, two additional features are added to the 0.45 chart: control points and a restricted zone. Control points function as master ranges through which gradations must pass. They are placed on the nominal maximum size, an intermediate size and the dust size.
The restricted zone resides along the maximum density gradation between the intermediate size (either 4.75 or 2.36 mm) and the 0.3 mm size. It forms a band through which gradations should not pass. Gradations that pass through the restricted zone have often been called “humped gradations” because of the characteristic hump in the grading curve that passes through the restricted zone. In most cases, a humped gradation indicates a mixture that possesses too much fine sand in relation to total sand. This gradation practically always
results in tender mix behavior, which is manifested by a mixture that is difficult to compact during construction and offers reduced resistance to permanent deformation during its performance life. Gradations that violate the restricted zone possess weak aggregate skeletons that depend too much on asphalt binder stiffness to achieve mixture shear strength. These mixtures are also very sensitive to asphalt content and can easily become plastic.

## Slide 10: Granulométrie des granulats selon Superpave
100
0
.075 .3 2.36 12.5 19.0
Pourcentage passant
Structure granulaire de formulation
tamis dimension (mm) Raised à 0.45 Power
Notes: The term used to describe the cumulative frequency distribution of aggregate particle sizes is the design aggregate structure. A design aggregate structure that lies between the control points and avoids the restricted zone meets the requirements of Superpave with respect to gradation. Superpave defines five mixture types as defined by their nominal maximum aggregate size:

## Slide 11: Désignations des dimensions des mélanges Superpave
Superpave nom max dimension max dimension
Désignation (mm) (mm)
37.5 mm 37.5 50
25 mm 25 37.5
19 mm 19 25
12.5 mm 12.5 19
9.5 mm 9.5 12.5
Notes: These are the five gradations developed for Superpave.

## Slide 12: Gradations
* Considérapportns:
- max. dimension < 1/2 AC lift Épaisseur
-
Dimension maximale plus grande
+ Augmente résistance
+ Améliore adhérence / résistance au glissement
+ Augmente Volume et Surface area de agg which Diminue nécessaire AC teneur
+ Améliore résistance à l’orniérage
+ Augmente problem avec ségrégation de particules
- Smaller max dimension
+ Réduit ségrégation
+ Réduit bruit de roulement
+ Diminue usure des pneus
Notes: Several factors need to be considered in selecting a desirable aggregate gradation. The maximum size of the aggregate needs to be at a minimum less than one half of the planned lift thickness. Current construction practices with Superpave gradations indicate that this needs to be changed to less than one-third of the lift thickness.
Larger maximum size aggregate gradations have several advantages such as improved aggregate interlock, improved skid resistance and improved rut resistance. Local availability of aggregates will usually dictate the largest size aggregate. Also, the larger maximum size gradations also tend to have more problems with gradation separation (segregation) during construction.

## Slide 13: Granulométrie cible
Fuseau granulométrique acceptable spécifié
La formulation du mélange sélectionne une formule de fabrication (JMF) située dans le fuseau et satisfaisant les critères de conception
Superpave
  5 nominales dimensions (37.5, 25, 19, 12.5, et 9.5 mm)
  Four tamis dimensions utilisé à Régler Supérieure et Inférieure Limites
  Staying out de Le zone restreinte is recommandé à Minimiser problèmes avec naturels sables
Notes: Target gradations are usually selected to meet an agency-specified gradation band. The selected gradation needs to meet the agency requirements as well as all other Superpave gradation and aggregate requirements.
At the present time, there are 5 Superpave gradation bands. Each uses 4 sieve sizes to set upper and lower limits on the gradation.
The restricted zone was originally included to help eliminate rounded natural sands. However, with the requirements on fine aggregate angularity, the need to stay out of the restricted zone is evaluated on a case by case basis (historical experience).

## Slide 14: Mélange des stocks de granulats
La formule de base pour combiner les stocks afin d’obtenir une granulométrie cible est :
p = Aa + Bb + Cc + ….
Où:
p = pourcentage de tapiserial Passant given tamis dimension
A, B, C, .. = pourcentage passant given tamis pour each agg.
a, b, c, … = decimal fraction de A, B, C, … à be utilisé
Notes: Once a target gradation or gradation band is selected, percentages of the aggregate stockpiles needed to produce an acceptable gradation are determined.
This is usually accomplished using a spreadsheet and a trial and error approach.

## Slide 15: Mélange des stocks de granulats
Tracer individuelles granulométries
Tracer spécification Limites
Can be utilisé pour initiale évaluation
  Can mélange be made à partir de availaboratoirele tapiserials?
  Identification de critiques tamis
  Est. essai proportions
Notes: The ability of a given set of aggregate stockpiles to meet particular gradation band requirements can be initially assessed by plotting the individual stockpile and gradation band requirements

## Slide 16: Toutes les combinaisons possibles se situent entre A et B
0.075 0.3 1 .18 4.75 9.5 12.5 19
tamis dimension, mm
pourcentage passant, %
points de contrôle pour
12. 5 nominales max. dimension
granulométrie A
granulométrie B
Notes: If the individual gradations bracket the gradation band, then it is possible to produce a combined gradation which will be within the gradation band. Determining the percentages will be a trial and error process.

## Slide 17: Aucune combinaison possible de A et B ne satisfera la spécification.
0.075 0.3 1 .18 4.75 9.5 12.5 19
tamis dimension, mm
pourcentage passant, %
points de contrôle pour
12. 5 nominales max. dimension
granulométrie A
granulométrie B
Notes: If the individual stockpile gradations are both either above or below the target gradation band, then there is no combination of the stockpiles which will produce an acceptable gradation.

## Slide 18: Toutes les combinaisons possibles passent par le point de croisement. Les mélanges contenant plus de A que de B seront plus proches de A
0.075 0.3 1 .18 4.75 9.5 12.5 19
tamis dimension, mm
pourcentage passant, %
points de contrôle pour
12. 5 nominales max. dimension
granulométrie A
granulométrie B
Notes: If the individual stockpile gradations cross, then the any combination of these stockpiles will have that same percentage for that particular sieve size.

## Slide 19: essai et Error Steps
Sélectionner critiques tamis dans mélange
Déterminer initiale proportions which will meet critiques tamis
vérifier calc. mélange against spécification
Régler if nécessaire et répéter above steps
Notes: Once it has been established that an acceptable gradation can be prepared using the designated stockpiles, these steps need to be followed to determine the desired percentages of each stockpile.

## Slide 20: Masses volumiques relatives des granulats mélangés
Une fois les pourcentages des stocks établis, les masses volumiques relatives combinées des granulats peuvent également être calculées
Notes: Remember, two specific gravity tests are needed. The results from these two tests need to be combined to obtain the specific gravity of the composite.

## Slide 21: Masses volumiques relatives combinées
G =
1
P1 + P2 + ……. Pn
100 G1 100 G2 100 Gn
Notes: This is the equation used for combining aggregate properties.

## Slide 22: Mélange des granulats
Raisons du mélange
  Obtenir une granulométrie souhaitée
  Un seul matériau naturel ou extrait en carrière ne suffit pas
  Il est économique de combiner des matériaux naturels et traités
Notes: We blend aggregates for these reasons.

## Slide 23: Mélange des granulats
Méthode numérique
  Essais et corrections
  Formule de base
Notes: There are two methods for blending aggregates. The most common is trial and error. The basic formula is not used.

## Slide 24: Mélange des granulats
P = Aa + Bb + Cc + ….
  Où:
  P = % Passant a given tamis pour mélangeed granulats A, B, C, …
  A, B, C, … = % tapiserial Passant a given tamis pour each granulat A, B, C, …
  a, b, c, … = proportions (decimal fractions) de granulats A, B, C, … à be utilisé dans mélange
Notes: This is the basic formula for blending.

## Slide 25: Mélange des granulats
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% utilisé
U.S. tamis
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
90
30
7
3
1
0
0
100
100
100
88
47
32
24
10
100
Notes: Example. Starting with two aggregates.

## Slide 26: Mélange des granulats
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% utilisé
U.S. tamis
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
45
15
3.5
1.5
0.5
0
0
100
100
100
88
47
32
24
10
100
50 %
50 %
Premier essai
(remember essai & error)
90
30
7
3
1
0
0
50
90 * 0.5 = 45
30 * 0.5 = 15
7 * 0.5 = 3.5
3 * 0.5 = 1.5
1 * 0.5 = 0.5
0 * 0.5 = 50
0 * 0.5 = 0
100 * 0.5 = 50
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
Notes: The first trial we will use 50% of each pile.

## Slide 27: Mélange des granulats
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% utilisé
U.S. tamis
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
45
15
3.5
1.5
0.5
0
0
100
50
50
44
23.5
16
12
5
50
50 %
50 %
90
30
7
3
1
0
0
50
95
65
47.5
25
16.5
12
5
100
100
100
88
47
32
24
10
100
Notes: This worked but the No. 50 sieve and the No 100 sieve are low.

## Slide 28: Mélange des granulats
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% utilisé
U.S. tamis
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
45
15
3.5
1.5
0.5
0
0
100
50
50
44
23.5
16
12
5
50
50 %
50 %
90
30
7
3
1
0
0
50
95
65
47.5
25
16.5
12
5
100
100
100
88
47
32
24
10
100
Essayons
et get
un peu plus près
du milieu des
valeurs cibles.

## Slide 29: Mélange des granulats
Agg. #2
Agg. #1
Blend
Target
Material
%
Passing
%
Passing
% utilisé
U.S. tamis
%
Batch
%
Batch
No. 4
No. 8
No. 16
No. 30
No. 50
No. 100
No. 200
3/8 “
80 - 100
65 - 100
40 - 80
20 - 65
7 - 40
3 - 20
2 - 10
100
27
9
2.1
0.9
0.3
0
0
100
70
70
61.6
32.9
22.4
16.8
7
70
70 %
30 %
90
30
7
3
1
0
0
30
97
79
63.7
33.8
22.7
16.8
7
100
100
100
88
47
32
24
10
100