## Slide 1: Cours C.03.06.01 Mélange bitumineux – historique de la formulation
Marek Pszczola
(présentation préparée sur la base des cours du prof. S. Romanoschi, États-Unis)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 4: Mélange bitumineux

## Slide 5: Essai « Pat »
Utilisé pour les asphaltes coulés d’environ 1900 au début des années 1920
Échantillons « Pat » d’asphalte coulé réalisés avec différentes teneurs en liant
Pressés contre un papier kraft brun :
- Tache importante – trop de liant
- Tache légère – trop peu de liant
- Tache moyenne – teneur optimale en liant

## Slide 6: Chaussée bitulithique
Warren Brothers a obtenu un brevet vers 1900
Gros granulats de 19 mm à 75 mm
Adapté aux roues à bandage métallique ou aux camions à pneus pleins dans les années 1900
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.

## Slide 7: Chaussée bitulithique
Des mélanges avec une dimension maximale de 12 mm ont été utilisés pour éviter les violations de brevet
Performance satisfaisante grâce à l’apparition du pneumatique
Adapté à la mise en œuvre mécanisée
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.

## Slide 8: Méthode Hubbard-Field
Développé dans 1920s à Déterminer optimal AC de sheet asphalt Surface et sable asphalt bases
éprouvette 2 inches diarespectéser par 1 inch Élevée forcé thrugueux a 1.75 inch diarespectéser orifice
Maximum charge reported as stabilité
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.

## Slide 9: Hubbard-terrain Méthode (Cont.)
First attempt à quantify stabilité at different teneur en liants
Modified dans 1950s à essai 6 inch HMA éprouvettes containing gros granulats
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.

## Slide 26: CHAUD mélanger béton bitumineux (HMA)mélanger Designs
Objectif :
  Développer un mélange économique de granulats et de bitume répondant aux exigences de conception
Historiques formuletion du mélange méthodes
  Marshall
  Hveem
New
  Superpave gyratory
Notes: The objective of HMA mix design is to develop an economical blend of aggregates and asphalt. In the developing of this blend the designer needs to consider both the first cost and the life cycle cost of the project. Considering only the first cost may result in a higher life cycle cost.
Historically asphalt mix design has been accomplished using either the Marshall or the Hveem design method. The most common method was the Marshall. It had been used in about 75% of the DOTs throughout the US and by the FAA for the design of airfields. In 1995 the Superpave mix design procedure was introduced into use. It builds on the knowledge from Marshall and Hveem procedures. The primary differences between the three procedures is the machine used to compact the specimens and strength tests used to evaluate the mixes. The current plan is to implement the Superpave procedures throughout the US for the design and quality control of HMA highway projects early in the next century. It appears that the Marshall method will continue to be used for airfield design for many years and that the Hveem procedure will continue to be used in California.

## Slide 27: Exigences communes
Teneur suffisante en bitume pour assurer une chaussée durable
Stabilité suffisante sous les charges de trafic
Vides d’air suffisants
  Supérieure limite à Éviter excessif environnementaux dommages
  Inférieure limite à perrespectéstre marge pour initiale densification en raison à trafic
Ouvrabilité suffisante
Notes: No matter which design procedure is going to be used the HMA mixture that is placed on the roadway must meet certain requirements.
The mix must have sufficient asphalt to ensure a durable, compacted pavement by thoroughly coating, bonding and waterproofing the aggregate.
Enough stability to satisfy the demands of traffic without displacement or distortion (rutting).
Sufficient voids to allow a slight amount of added compaction under traffic loading without bleeding and loss of stability. However, the volume of voids should be low enough to keep out harmful air and moisture. To accomplish this the mixes are usually designed by 4% VTM in the lab and compacted to less than 7% VTM in the field.
Enough workability to permit placement and proper compaction without segregation.

## Slide 28: Méthode de formulation Marshall
Développé par Bruce Marshall de Mississippi Élevéeway Department (1939)
Corps de Engineers conducted study dans 1943
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.

## Slide 29
Besoin pour a portable appareil à design et Contrôler HMA pour airterrain chaussées
Laboratoire compactive effort Développé à simuler terrain densité
Base pour sélection optimal teneur en liant
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.

## Slide 30
FORMULATION MARSHALL
Analyse de la densité et des vides
Essai de stabilité et de fluage

## Slide 31: Marshall formuletion du mélange
Développé par Bruce Marshall pour Le Mississippi Élevéeway Department dans Le late 30’s
WES began à study it dans 1943 pour WWII
  Evaluated compactage effort
    No. de bbassess, foot design, etc.
    Decided sur 10 lb.. Hammer, 50 bbassess/side
    4% vides Après trafic
initiale critères were établired et upgranulométrie pour accrues tire pressures et charges
Notes: Point out that the criteria has been modified since initial development; but, the basic process is the same as it was when it was initially developed.

## Slide 32: Marteau Marshall automatique
Notes: This picture is of automatic hammers. There are also hand held hammers. The key is that the base for the mold has to be solid.

## Slide 33: Marshall formuletion du mélange
Sélectionner et tester les granulats
Sélectionner et tester le bitume routier
  Établir les températures de malaxage et de compactage
Développer des mélanges d’essai
  Chauffer et mélanger le bitume routier et les granulats
  Compacter l’éprouvette (diamètre 100 mm)
Notes: This slide outlines the major steps in the development of a Marshall mix design.

## Slide 44: Stabilité et fluage Marshall
Notes: This is a Rainhart stability device. It uses a chart recorder to document the load and the flow (deformation of the specimen).

## Slide 50: Températures de malaxage/compactage
.1
.2
.3
.5
1
10
5
100
110
120
130
140
150
160
170
180
190
200
Température, °C
Viscosité, Pa·s
Plage de compactage
Plage de malaxage
Notes: To establish mixing and compaction temperatures it is necessary to develop a temperature viscosity chart. This can be done by determining the viscosity at two different temperatures - generally 135 C and 165 C. These two viscosities are then plotted on the graph above and a straight line is drawn between the two points.
The desired viscosity range for mixing is between 0.15 and 0.19 Pa-s and 0.25 and 0.31 Pa-s for compaction. Appropriate mixing and compaction temperatures are selected as the temperature where these viscosity requirements are met. This information can be obtained from the suppliers. In many DOTs this information is developed during the mix design process.
If using modified binders - it is recommended that you should contact the supplier to determine the mixing and compaction temperatures.

## Slide 51: Critères de formulation Marshall
Trafic léger Trafic moyen Trafic lourd
ESAL < 104 10 4 < ESAL< 10 ESAL > 106
compactage 35 50 75
stabilité N (lb.) 3336 (750) 5338 (1200) 8006 (1800)
fluage, 0.25 mm (0.1 dans) 8 à 18 8 à 16 8 à 14
vides d’air, % 3 à 5 3 à 5 3 à 5
vides dans Mineral Agg.
(VMA) Varies avec granulat dimension
Notes: The criteria on this slide is that recommended by The Asphalt Institute. Most DOTs have their own requirements and they may vary some from that noted here.

## Slide 52: Minimum VMA exigences
Notes: As the aggregate size increases the VMA requirement will drop.

## Slide 53: Marshall formuletion du mélange Essais
Heights
  Utilisé pour corriger les mesures de stabilité
Masse volumique relative apparente de l’échantillon compacté
Masse volumique relative maximale du mélange non compacté
Stabilité et fluage
  60oC water bain (30 à 40 minutes)
  50 mm/min chargement vitesse
  Charge maximale = stabilité non corrigée
  Déformation verticale correspondante = fluage
Notes: This slide shows the mixture tests required to complete a Marshall mix design.
In the stability calculations there is an assumption that the height is 2 1/2 inches. If the height is different there is a correction procedure for the Marshall Stability that must be followed.
The bulk specific gravity along with the maximum specific gravity is used in the volumetric calculations.
The Marshall procedure calls for a strength test - the Marshall stability and flow test.

## Slide 54: Marshall Design Utilisation de DataAsphalt Institute procédure
Vides d’air, %
Teneur en bitume, %
Stabilité
Teneur en bitume, %
Unit Wt.
Teneur en bitume, %
Teneur optimale cible en bitume = moyenne
4%
Notes: There are a number of plots used to analyze Marshall data:
Air voids vs asphalt content: goes down as AC content increases
Stability vs asphalt content: goes up to a peak and then drops off
Unit Wt vs asphalt content: This is similar to a moisture density relationship for soils. The unit wt increases until the asphalt cement acts like an extender rather than a lubricant.

## Slide 55: Marshall Design Utilisation de DataAsphalt Institute procédure
Fluage
Teneur en bitume, %
VMA, %
Teneur en bitume, %
Utiliser la teneur optimale cible en bitume pour vérifier si ces critères sont respectés
Limite inférieure
Limite supérieure
Minimum
OK
OK
Notes: The other two curves are:
Flow versus ac content: This will initially drop and then increase.
VMA versus ac content: This will initially drop and then rise. It is desirable to design mixes on the down side of this curve. They are easier to control.

## Slide 56: Marshall Design Utilisation de DataNAPA procédure
Vides d’air, %
Teneur en bitume, %
cible optimal asphalt teneur =
la teneur en bitume correspondant à 4 % de vides d’air
4%
Notes: The design asphalt content is defined as the asphalt content that will produce 4% air voids.

## Slide 57: Marshall Design Utilisation de DataNAPA procédure
Stabilité
Teneur en bitume, %
La stabilité cible est vérifiée
OK
Notes: After the design asphalt content is picked, the other properties are checked.

## Slide 58: Marshall Design Utilisation de DataNAPA procédure
Fluage
Teneur en bitume, %
VMA, %
Teneur en bitume, %
Utiliser la teneur optimale cible en bitume pour vérifier si ces critères sont respectés
Limite inférieure
Limite supérieure
Minimum
OK
OK

## Slide 59: Marshall Design Méthode
Avantages
  Attention portée aux vides, à la résistance et à la durabilité
  Équipement peu coûteux
  Facile à utiliser pour le contrôle de production et la réception
Inconvénients
  Méthode de compactage par impact
  Ne prend pas en compte la résistance au cisaillement
  Charge perpendiculaire à l’axe de compactage
Notes: One of the strengths of the Marshall method is its attention to density/voids analysis. This ensures that the important volumetric properties of the mix are at their optimum levels to achieve a durable HMA pavement. Another advantage is that it required equipment that was relatively inexpensive and very portable. This lead to its use for quality control operations. Unfortunately the impact method of compaction does not simulate densification that occurs under traffic in a real pavement. The strength parameter does not adequately measure the shear strength of the HMA.

## Slide 60: Formulation Hveem

## Slide 61: Méthode de formulation Hveem
Francis Hveem Développé pour California DOT dans mid 1920’s
limiteées Utiliser
  Principalement dans West coast states
Addresses similaires design Considérapportns as Marshall
Prend en compte asphalt absorption par granulat
Notes: As a resident engineer in California Francis Hveem began to work with “oil mixes” in the late 1920s. Hveem noticed in his work that there was a relationship between the gradation of the aggregate and the amount of oil needed to develop a consistent mix. He found a way of determining the surface area of the gradations and using that with a “kerosene equivalent test” to determine absorption of the asphalt he developed a design procedure. But, he noticed that the procedure did not insure rutting resistance. He decided that another test was needed to evaluate the ability of the mix to resist shear forces applied by wheel loads. This led to the development of the Hveem stabilometer.
The system has been used primarily in the Western states and is still used in California.

## Slide 62: Méthode de formulation Hveem
Sélectionnerion et essaiing de granulats
Sélectionnerion et essaiing de liants
Centrifuge kerosene equivalent (CKE)
  Surface capacité de granulat
  Estitapise optimal asphalt teneur
Notes: A thorough evaluation of the aggregates and binders is conducted. The procedure calls for determining an approximate asphalt content by the Centrifuge Kerosene Equivalent test and then subjecting specimens at that asphalt content, and a higher and lower asphalt contents to a stability test.

## Slide 63: Méthode de formulation Hveem
Utiliser kneading compactor à préparer éprouvettes
Déterminer stabilité avec Hveem stabilorespectéser
  Évalue horizontale defortapision sous axiale charge
  éprouvette chargeed along axe de compactage
Visuelle observation, volumétrie, et stabilité utilisé à Sélectionner optimal asphalt teneur
Notes: Samples are made using the California Kneading Compactor. The stability is then determined using the Hveem stabilometer.

## Slide 64
Compacteur à pétrissage Hveem

## Slide 65: Stabilomètre Hveem
Notes: The procedure for the Hveem Stabilometer test is:
Heat the specimens to 60 C.
A test load is applied to the specimen at the rate of 1.3 mm per minute and gauge readings are made at 2.22, 4.45 increments up to 26.7 kN.
Turn the displacement pump handle clockwise rapidly until the pressure is 690 kPa. Read the Ames dial and record in 0.25 mm units.
The Stabilometer value is determined from that data.

## Slide 72: Méthode de formulation Hveem
Stabilité
Teneur en bitume, %
Vides d’air, %
Teneur en bitume, %
VMA
Teneur en bitume, %
Lourd trafic = 37 stabilité min.
Moyen = 35 min.
Léger = 30 min.
Minimum
Minimum
Notes: As the asphalt content increases the Hveem Stability decreases, the air voids decrease and the VMA decreases to a point and then increases. As the traffic level increases the stability requirement increases.

## Slide 73: Méthode de formulation Hveem
Step 1
Design Series
Step 2
Flushing
Step 3
Min. stabilité
Step 4
max. AC avec 4% vides
Notes: The following steps are followed in determining the design asphalt content:
Step 1 - Record the four asphalt contents used for preparing the mix specimens. Record them in order of increasing amount from left to right.
Step 2 - Select from Step 1 the three highest asphalt contents that do not exhibit moderate or heavy flushing and record them in step 2.
Step 3 - Select from Step 2 the two specimens that provide the specified minimum stability and enter them in step 3.
Step 4 - Select from Step 3 the highest asphalt content that provides at least 4% air voids.

## Slide 74: Hveem formuletion du mélange
Avantages
  Attention à vides, résistance, durabilité
  Kneading compactage similaires à terrain
  Strength pararespectéser direct indication de interne friction component de cisaillement résistance
Inconvénients
  équipement expensive et Pas easily portable
  Pas large Plage dans stabilité mesures
Notes: The Hveem method has two real advantages. First, the kneading compactor of laboratory compaction is thought by most engineers to simulate the densification characteristics of HMA in the field. Second the Hveem stability is a direct measurement of the internal friction component of shear strength. It measures the ability of a test specimen to resist lateral displacement from application of a vertical load.
The disadvantage of the Hveem procedure is that the testing equipment is that the equipment is expensive - particularly the kneading compactor and stabiliometer. There is not a wide range in the stability results.

## Slide 75: Hveem formuletion du mélange
1984 Survey - 75% states utilisé Marshall, 25% states utilisé Hveem
Les méthodes Marshall et Hveem sont toutes deux empiriques
Elles ne sont plus suffisantes pour les charges de trafic accrues
Une méthode rationnelle de formulation du mélange, fondée sur des principes d’ingénierie, est nécessaire

## Slide 76: Méthode de formulation Superpave
Résultat du programme stratégique de recherche routière (SHRP)
Programme de recherche de 5 ans et 50 millions de dollars, achevé en 1992
Formulation volumétrique utilisant un compacteur giratoire
Mise en œuvre par 2000 par most states
Notes: Hence, there is a need for a mechanical test which can tell us whether the designed mix is resistant to rutting. It should be able to proof test the mixes and tell us whether a mix satisfies a definite criteria and passes or fails the torture test. This test should be a laboratory test method so that it can be used on designed mixes, and it should be a simple test method so that it can be used routinely by the folks who actually build our pavements.