## Slide 1: Course C.03.06.02 Distresses of pavements
Marek Pszczola
(presentation was prepared on the basis of lectures prof. S. Romanoschi, USA)

## Slide 2: Road Transportation Systems Engineering Development in the Sub-Saharan Africa – Modern EU Master Programme & Capacity Building

## Slide 6: Basic Requirements for Flexible Pavements
Drainage, drainage, drainage
Sufficient thickness and internal strength to carry expected traffic loads
Adequately dense to prevent penetration of moisture from underneath, sides, and surface
Top surface which is smooth; waterproof; skid resistant; resistant to wear, distortion, and deterioration by weather and deicing chemicals

## Slide 8: Typical Distresses in Asphalt Pavements
Distress Mode
Fracture
Distortion
Distress Manifestation
Cracking
load associated (fatigue)
non-load associated
reflection
Spalling
Permanent Deformation
densification
creep (rutting/shoving/ corrugations)
swelling/frost
Slippage

## Slide 9: Typical Distresses in Asphalt Pavements (Cont.)
Distress Mode
Disintegration
Other
Distress Manifestation
Stripping
Raveling
Scaling
Potholes
Reduced skid resistance
Riding quality-roughness

## Slide 10: Cracking of Asphalt Pavements: Causes

## Slide 11: Load Associated (Fatigue) Cracking
Also called alligator or map cracking
Loads too heavy for the pavement structure
Too many repetitions of load
Inadequate support (pavement layers/subgrade)
Poor drainage
Very stiff binder in surface course
Occurs in wheel path, potholes develop in advanced stage

## Slide 12: Non-Load Associated (Thermal) Cracking
Transverse cracks occur at regular intervals
Asphalt too stiff at low service temperatures
Rapid chilling of the road surface
Highly temperature susceptible asphalt
Subgrade type (more on sandy)
Age of the pavement

## Slide 13: Longitudinal Cracking
Occurs parallel to the center line of roadway
Center Line Joint
Joint between adjacent lanes
Density gradient across the joint
Low density - low tensile strength
Edge Cracking
Lack of lateral (shoulder) support
Settlement of widened pavement
Poor drainage (ditches)

## Slide 14: Block Cracking
Both transverse and longitudinal cracking
Most often on low volume roads/parking lots
Thixotropic hardening (structuring) of asphalt binder

## Slide 15: Reflection Cracking
Discontinuities in the underlying layers propagate through the HMA surface due to movement of cracks
Discontinuities
Cracks or joints in underlying PCC pavement
Cracks in soil-cement base course
All types of cracks in the existing HMA pavement
Causes
Thermal (movement of joints/cracks)
Load

## Slide 16: Slippage Cracking
Associated with slippage mechanism
Poor bond between the surface and underlying layer
Too much or too little tack coat
Steep grades/intersections
Acceleration/braking exert surface traction forces
U-shaped

## Slide 17: Rutting
Lack of adequate subgrade support
Unstable HMA course(s)
  Poor mix design
  Rounded aggregate
  Excessive binder
Stripping
  Lack of bond between HMA courses
  Unstable surface course mix
  Braking and accelerating action near intersections
Corrugations

## Slide 18: Stripping
Breaking of adhesive bond between the aggregate surface and asphalt binder usually in presence of moisture
Inadequate pavement drainage system
Mixes with excessive air voids (poor compaction), and low asphalt content
Incompatible aggregate surface and asphalt binder, asphalt binder displaced by water
Excessive pore pressure induced by traffic
Spontaneous emulsification of binder by water

## Slide 19: Raveling
Progressive disintegration of HMA surface as a result of dislodgment of aggregate particles in the mix
Lack of sufficient cohesion due to low in-place density
Lack of fines in the matrix, especially in coarse, segregated areas
Aging of asphalt binder

## Slide 20: Skid Resistance
Friction between the tire and road surface. Quantified by Friction Number (FN). Critical when surface is wet.
Causes for Low FNs
Flushing/bleeding of HMA surface
Inadequate microtexture
- aggregate prone to polishing
Inadequate macrotexture
- no drainage channels
- causes hydroplaning
- important at high speeds